[image: image2.jpg]


BH-2(HF)
	LOW SMOKING, HALOGEN FREE, FLAME 

RETARDANT HEAT SHRINKABLE TUBING

SHRINK RATIO 2:1 
Features/Applications

As a kind of totally environmental friendly heat-shrinkable tube, it is made
with specially designed halogen free polyolefin. It produces neither toxic 
smoke nor harmful substance when burning, which meets the growing demand 
of environmental protection all over the world. Except the common fine 
physical and chemical specifications, the tube also shows excellent 
flame-retardant, insulation, low temperature shrinking and flexible 
properties and  thus be widely used in electron, communication and 
automobile industry.
(  Minimum shrink temperature: 65℃ 

(  Minimum fully recovery temperature: 95℃ 

(  Operating temperature: -55℃~+105℃
(  Standard color: Black, White, 
    Other color are available on request
	

	
Property
Test Method
Typical Data
Operating temperature
IEC 216
-55 to +105℃
Tensile strength
ASTM D 2671
>10.4MPa

Elongation at break
ASTM D 2671
200%

Longitudinal shrinkage
UL224

±3%

Eccentricity
ASTM D 2671

≤30%

Heat shock
250℃/4hrs
No crack
No dropping

Heat aging

Tensile strength

Ultimate elongation

136℃/168hrs

9.0MPa

>150%

Flammability
SAE-AMS-DTL-23053/5

Pass

	
Normal Size
(mm)
As supplied(mm)
After recovered (mm)
Standard length
(m/spool)
Inside
diameter
(mm)
Wall thickness
(mm.)
Inside diameter (Max.)
Wall 
thickness
(mm.)
Φ1.0

1.5±0.2

0.18

0.50

0.33

200

Φ1.5

2.0±0.2

0.18

0.75

0.36

200

Φ2.0

2.7±0.2

0.25

1.00

0.44

200

Φ2.5

3.1±0.2

0.25

1.25

0.44

200

Φ3.0

3.7±0.3

0.25

1.50

0.44

200

Φ3.5

4.0±0.3

0.25

1.75

0.44

200

Φ4.0

4.7±0.3

0.25

2.00

0.44

200

Φ5.0

5.6±0.3

0.25

2.50

0.56

100

Φ6.0

6.8±0.3

0.25

3.00

0.56

100

Φ7.0

7.7±0.3

0.25

3.50

0.56

100

Φ8.0

8.8±0.3

0.30

4.00

0.56

100

Φ9.0

9.8±0.3

0.30

4.50

0.56

100

Φ10

10.7±0.4

0.30

5.00

0.56

100

Φ11

11.7±0.4

0.30

5.50

0.56

100

Φ12

12.7±0.4

0.30

6.00

0.56

50

Φ13

13.7±0.4

0.30

6.50

0.65

50

Φ14

14.7±0.4

0.35

7.00

0.69

50

Φ15

15.7±0.5

0.35

7.50

0.69

50

Φ16

16.7±0.5

0.35

8.00

0.69

50

Φ18

19.0±0.5

0.40

9.00

0.80

50

Φ20

21.4±0.5

0.40

10.00

0.80

50

Φ22

23.4±0.6

0.45

11.00

0.80

50

Φ25

26.5±0.8

0.45

12.50

0.90

50

Φ28

29.5±0.8

0.45

14.00

0.90

50

Φ30

31.5±0.8

0.45

15.00

0.90

50

Φ35

36.5±0.8

0.50

17.50

0.90

50

Φ40

42.0±0.8

0.50

20.00

1.00

50

Φ50

52.0±0.8

0.50

25.00

1.00

50

Φ60

62.0±1.0

0.50

30.00

1.00

30

Φ70

72.0±1.0

0.50

35.00

1.20

30

Φ80

82.0±1.0

0.55

40.00

1.20

30

Φ100

102.0±1.0

0.55

50.00

1.30

30

Φ125

126.0±1.0

0.55

60.00

1.30

15

Φ150

152.0±1.0

0.55

75.00

1.30

15

Special size, cut pieces are available on request.
                    


[image: image1.jpg]



THIN WALL TUBING                                     FLYPOWER











Technical Data





Product Dimensions (mm)








